## Slide 1: Design Rule check

## Slide 2: Design Rules
Substrate thickness: recommendation ~300µm
Mold material: Hitachi GE100LFCS-K
Mold cap thickness: 670µm
Topology in die attach area max ~10-20µm
Topology in wire bond area <10µm
Package Outline check
  Dicing kerf in layout 220µm = dicing blade widths 220µm (Backup: 200µm blade widths)
50µm line in ficucial okay
Dicing kerf – check with Maciej
Adhesion of mold compound
  Solder Stop area as big as possible to get a good mold ahesion
Risk of „leakage“,...
  Avoid dicing through metal within PCB layer stack
    Dicing kerf in layout 220µm -> Metal pull back 80µm  300µm metal free zone in dicing kerf  40µm on each side
Bonding
  No via hole allowed in (wire) bond area
LFBGA fiducial – template from LFBGA 160-2
  Dicing fiducial adapted to =150µm layout dimension (otherwise higher costs)
  Accretech dicer is checking 300x400µm windows to adjust dicing channel
  PIN1 on device / PIN1 on substrate

## Slide 3: Layout from Maciej Jankowski

## Slide 4: LFBGA Assembly Process @ RBG Fast Prototyping
Shipment from Hofmann Leiterplatten RBG
Die-attach
Wirebond
Molding
Laser marking
Singulation
Single layout by IFX
PCB layout done by HLP
Requirement for PCB to do BE assy? Passives attached at HLP
Die-attach
Material: Loctite hybrid silver 8068TB (must)
Bond line thickness: 10-25µm
Wirebonding
25µm Au wire - ball on stitch (Chuck!?)
Molding
Material: Hitachi GE100LFCS-K (must)
Transfer mold – use existing mold tooling
0.8mm/0.9mm mould cap
Laser Marking
Serialisation/Identification of individual parts
DoE variants
Singulation
Dicing blade/parameters
Blade width 240µm
Shipment: Frame
A
B
C
D
RBG Assy

## Slide 5: RF-MINIPAC T9501A - Laser Marking
Laser Marking Pattern
  1. row: PIN 1 orientation! + Infineon
  2. row: “LF0001-T9501A-V2”  [Leadframe Version]-[Die Basictype]
  3. row: “A-0001”  [Panel Section]-[Unit Count]
  4. row: “ES” + “Date code”
A
B
C
D
Panel Section ID
216 pieces per panel
4x9x6
187.5mm
50mm
PIN1 marking soldering side  corner cut available
Bottom right
LF0001-T9501A-V2
A-0002
ED 2140

## Slide 6
PIN1 on device